MARGEN PREMIUM MARINE DEO SAE 30 API CF are new generation lubricating oils specially developed for use in heavy duty slow speed crosshead diesel engines.   It is formulated from high quality base stock and additives to provide the necessary performance characteristics for lubrication of marine diesel engines.

They are   compounded   with   a   high performance zinc and calcium additive 
system   to   provide   superior   oxidation resistance, deposit control, and anti-wear protection for engine components in severe services.

APPLICATIONS:

MARGEN PREMIUM MARINE DEO SAE 30 API CF are recommended for lubrication of crosshead marine and stationary diesel engines and meets the requirements of the major marine engine manufacturers.

BENEFITS:

- Superior oxidation stability prevents sludge, varnish and carbon deposits.

- Zinc formula protects key engine components from corrosion and wear.

- High alkalinity retention maximizes oil service life.

- Trunk pistons (TP) or engine cylinder (EC) service.

- Reduces maintenance by controlling deposits in the ring belt and intake ports.

| TECHNICAL DATA |
| --- |
| SAE GRADE | 30 |
| Sp. Gravity @ 15°C | 0.85-0.91 |
| Kinematic Viscosity @ 40°C cSt | 90-100 |
| Kinematic Viscosity @ 100°C cSt | 10.50 – 11.50 |
| Viscosity Index | 95 -100 |
| TBN mgKOH/gm | 5 – 6 |
| Flash Point°C | 240 -260 |
| Pour Point°C | -12 to - 18 |

Health and Safety:  Based on available information, this product is not expected to produce adverse effects on health when used for the intended application, following the recommendations provided in the Material Safety Data Sheet (MSDS). MSDSs are available upon request.   This product should not be used for purposes other than its intended use.  If disposing of used product, take care to protect the environment.

Due to continual product research and development, the information contained herein is subject to change without notification.   Typical Properties may vary slightly.

Published by General Petroleum GmbH Frankfurt, Germany

Last Updated on: August 2012